## Slide 1
Improving RRAM Performance through Uncertainty Quantification
Ziyan Liao1, Zhiheng Huang1, Min Xiao1, Yuezhong Meng1, Hui Yan2 and Yang Liu3
1 The Key Laboratory of Low-carbon Chemistry & Energy Conservation of Guangdong Province,
and School of Materials Science and Engineering, Sun Yat-sen University, Guangzhou, China
2 School of Computer Science and Engineering, Sun Yat-sen University, Guangzhou, China
3 School of Electronics and Information Technology, Sun Yat-sen University, Guangzhou, China
liaozy9@mail2.sysu.edu.cn

## Slide 2
Contents
1
Background
2
Model and Method
RRAM: structure, advantages and challenges
The filamentary switching mechanism
The geometry and PDEs
Uncertainty quantification method
Model implementation
3
Results
Achieving an increase in on/off ratio
Reducing the SET and RESET power consumption

## Slide 3
Background
RRAM: a promising candidate for next-generation memory
Characteristics
High switching speed (85 ps)
Simple structure
Scalability
CMOS compatibility
Non-volatility
Low power consumption
Cycling endurance
……
OFF
ON
Pt / AlN / Al
Choi et al., Adv. Funct. Mater. 26, 5290 (2016)
© CrossBar, Inc.
2.2nm
2.1nm
Pi et al., Nat. Nanotechnol. 14, 35 (2019)

## Slide 4
RRAM: challenges
Simple structure but rich materials, physics, chemistry and electrical issues
Challenges
The continuous reduction of feature size may affect the reliability of RRAM devices
No quantitative relationship between material properties and RRAM device properties
……
How to solve?
The uncertainty of material microstructure is particularly important
The Uncertainty quantification (UQ) module in COMSOL Multiphysics is an ideal platform
A response surface in UQ module

## Slide 5
RRAM: switching mechanism
The switching mechanism is based on the formation and break of conductive filament (CF) in the oxide layer
The model consists of four modules corresponding to ON and OFF states and SET (OFF→ON) and RESET (ON→OFF) switching process
OFF: insulation
High resistance
SET: OFF→ON
Formation of CF
RESET: ON→OFF
Breaking of CF
ON: conducting
Low resistance

## Slide 6
RRAM: model
Electro-thermo coupled PDEs
OFF / ON | SET / RESET
Electric Currents module | 
Heat Transfer in Solids module | 
Multiphysics module | 
OFF / ON | SET / RESET
Electric Currents module | 
Heat Transfer in Solids module | 
Multiphysics module | 
D. Niraula et al., J. Appl. Phys. 124, 174502 (2018)
Geometry
TiN / Hf / HfO2 / TiN RRAM device is modeled in COMSOL Multiphysics

## Slide 7
UQ method
Quantities of interest (QoIs)
  The on/off ratio
  The power consumption of SET and RESET processes
Input parameters
  Evaluate the importance of 24 input parameters
Parameter | Value | Parameter | Value | Parameter | Value | Parameter | Value | Parameter | Value
 | -0.05 |  | 13310 kg/m3 |  | 144 J/(kg·K) |  | 10-9 S/m |  | -106
 | 0.05 |  | 5220 kg/m3 |  | 545 J/(kg·K) |  | 10 S/m |  | -106
 | 5 nm |  | 2203 kg/m3 |  | 703 J/(kg·K) |  | 7000 S/m |  | 3.9
 | 3.1 kΩ |  | 10000 kg/m3 |  | 120 J/(kg·K) |  | 0.5 W/(m·K) |  | 25
 | 150 μA |  | 12000 kg/m3 |  | 140 J/(kg·K) |  | 1.38 W/(m·K) |  | 
Parameter | Value | Parameter | Value | Parameter | Value | Parameter | Value | Parameter | Value
 | -0.05 |  | 13310 kg/m3 |  | 144 J/(kg·K) |  | 10-9 S/m |  | -106
 | 0.05 |  | 5220 kg/m3 |  | 545 J/(kg·K) |  | 10 S/m |  | -106
 | 5 nm |  | 2203 kg/m3 |  | 703 J/(kg·K) |  | 7000 S/m |  | 3.9
 | 3.1 kΩ |  | 10000 kg/m3 |  | 120 J/(kg·K) |  | 0.5 W/(m·K) |  | 25
 | 150 μA |  | 12000 kg/m3 |  | 140 J/(kg·K) |  | 1.38 W/(m·K) |  | 
The 24 input parameters
D. Niraula et al., J. Appl. Phys. 124, 174502 (2018)

## Slide 8
UQ analysis
Inputs
Sensitivity
analysis
Sobol diagram
2
Inputs
Reliability
analysis
4
Probability
Inputs
MOAT
screening
MOAT scattergram
1
Inputs
Uncertainty
propagation
Predicted output
3

## Slide 9
Model implementation
Focusing on two key performance indicators (KPIs) for RRAM devices
The on/off ratio
The power consumption of SET and RESET processes
LiveLink for MATLAB
MATLAB function
The four modules of RRAM are constructed in COMSOL
Use MATLAB to integrate these modules seamlessly and extract KPIs as outputs
To integrate KPIs into QoIs of UQ analyses, corresponding MATLAB functions are created within the COMSOL Desktop
Start COMSOL server manually
Conduct UQ and optimization

## Slide 10
Result: on/off ratio
The on/off ratio determines the ability to distinguish between “0” and “1” states
  The on/off ratio can be calculated:
To analyze the impact of cycle characteristics, RRAM devices that have been operated for 1 and 5 cycles were screened to obtain the MOAT scattergram
1 cycle
5 cycles
The vertical axis represents the interaction and nonlinear effects between parameters
The horizontal axis represents the overall impact of a parameter on the output

## Slide 11
Result: on/off ratio
Adjust key parameter values to improve on/off ratio
  At the initial setting, the on/off ratio is between 4 and 6, and there is no sign of degradation after 3700 cycles
  With the following parameter setting: = 0.07, = −0.07, = 105 S/m and = 3 nm, the on/off ratio can be improved by 13 times, and after 500 cycles, the on/off ratio can still be improved by nearly 10 times
At the initial setting
3700 cycles
Adjusting key parameters
500 cycles

## Slide 12
Result: power consumption
The power consumption is defined as the product of the current and voltage switching to the SET and RESET processes
Perform sensitivity analysis for and respectively to get the Sobol diagram
The LHS column of each parameter represents the first-order Sobol indices, indicating the sensitivity when the parameter is varied alone.
The RHS column of each parameter represents the total Sobol indices, indicating the contribution of that parameter to the overall sensitivity.

## Slide 13
Result: power consumption
KDE plot of
KDE plot of
Adjust key parameter values to decrease power consumption
  With the parameter setting: = −0.07, = 105 S/m, = 9 nm and = 1.5 W/(m·K), are reduced by 32%, and the reliability analysis indicates a probability of 0.158
  Similarly, with the parameter setting: = −0.07, = 105 S/m, = 3 nm and = 3.5 kΩ, are reduced by 38%, and indicates a probability of 0.186
  By uncertainty propagation, the KDE plots are obtained to predict the probability density curves for and

## Slide 14
By adjusting the parameters, the on/off ratio is increased by about 13 times, and are reduced by about 32% and 38%, respectively, and reliability analysis indicates a more practical and achievable level of performance enhancement
2
1
By using UQ methods, the influence of material uncertainty on RRAM on/off ratio and power consumption is discussed, and the probability distribution relationship between input parameters and device performance is predicted
Conclusions

## Slide 15
Thanks for your attention!