## Slide 1: Rubbing-Induced Metal Ignition in Oxygen-Rich Turbomachinery
M. French, Z. Cordero
Gas Turbine Laboratory, MIT

## Slide 2
Rubbing in turbomachinery can escalate to loss of entire spacecraft.
Antares Orb-3 Launch Failure — NASA/Joel Kowsky, 2014
Antares Orb-3: ISS Resupply Mission
outcome - explosion from metal fire destroyed entire spacecraft and cargo within seconds
metal fire origin - friction from rubbing in turbopump with oxygen-rich environment
ongoing risk - oxygen-rich turbomachinery is necessary to achieve performance goals for next-generation rocketry
Reference [1]
2

## Slide 3
Aerojet AJ26 Rocket Engine - NASA
turbopump
rotor
blades
casing
model turbine
+
ignition
risk
turbine
rub
hot, high pressure O2
=
Why are oxygen-rich turbopumps vulnerable to frictional ignition?
3
stator

## Slide 4
Simulations bridge the gap between testing and reality.
COMSOL
References [2, 6]
frictional heating
casing
blades
T = 750 K P = 60 MPa V = 250 m/s
T = 300 K P = 25 MPa V = 22 m/s
laboratory testing
turbomachinery
4

## Slide 5
Model simulates ignition and implements mitigation strategies
imported CFD fields
frictional ignition model
ignition prediction
workflow
limiting cases
mitigation strategies
blade ignition
casing ignition
material selection, operating conditions, tip geometry
5

## Slide 6
References [3]-[7]
blade
casing
Heat Transfer in Solids (ht)
initial conditions
local CFD fields
oxidation
friction
convection
COMSOL model implements transient frictional heating
6

## Slide 7
Blade heating from continuous rub
1600 K
1400 K
1200 K
1000 K
800 K
temperature (K)
time (μs)
7

## Slide 8
Blade ignition from continuous rub
1600 K
1400 K
1200 K
1000 K
800 K
temperature (K)
time (μs)
8

## Slide 9
Using ignition threshold as a design tool
ignition threshold
quenching
ignitable
9
rapid quenching
rapid ignition
marginal quenching
marginal ignition

## Slide 10
Casing ignition from periodic rubbing
1600 K
1400 K
1200 K
1000 K
800 K
temperature (K)
at indicated point
time (μs)
10

## Slide 11
Preventing ignition through materials selection
MK500
IN718
References [6], [8]-[10]
11

## Slide 12
Moving from failure to iterative design
represent in-engine conditions
predict when and where ignition occurs
screen mitigations prior to destructive testing
design rub-tolerant, ignition-resistant engines
12

## Slide 13
Acknowledgements
We thank Roger Hou (MIT) for initial development of the turbine design used in the CFD simulations.
We thank our collaborators Tobias Brandvik (Turbostream Norway) for contributions to turbine design and CFD, and Andres Garcia Jimenez (The Aerospace Corporation) for contributions to frictional-ignition modeling.
High-fidelity CFD simulations used resources provided by Sigma2 — the National Infrastructure for High-Performance Computing and Data Storage in Norway.
[1] NASA Independent Review Team, Orb-3 Accident Investigation Report, 2015. [2] Wabel, T. M., et al., “Frictional Ignition Testing of Metals in Oxygen up to 24.1 MPa,” AIAA 2023-1491, 2023. [3] Kennedy, T. C., et al., Wear 261, 932–936, 2006. [4] Bosman, R. & de Rooij, M. B., J. Tribol. 132, 021401, 2010. [5] Bos, J. & Moes, H., J. Tribol. 117, 171–177, 1995. [6] Garcia Jimenez, A., Tribochemistry of Frictional Ignition in High Pressure Oxygen, Ph.D. thesis, MIT, 2025. [7] Davis, G. A. & Clough, R. C., Blade Tip Rubbing Stress Prediction Final Report, Rocketdyne, 1991. [8] Pottlacher, G., et al., Scand. J. Metall. 31, 161–168, 2002. [9] Agazhanov, A. Sh., et al., “Thermophysical Properties of Inconel 718 Alloy,” XXXV Siberian Thermophysical Seminar, 2019. [10] Special Metals Corp., MONEL® Alloy K-500, Publication SMC-062, 2004.
Selected References
13

## Slide 14
Moving from failure to iterative design
represent in-engine conditions
predict when and where ignition occurs
screen mitigations prior to destructive testing
design rub-tolerant, ignition-resistant engines
14

## Slide 15: BACKUP SLIDES

## Slide 16
Boundary Heat Flux
interfacial heat flux (friction)
exposed surface heat flux (oxidation, convection)
Arrhenius oxidation regime. Assume protective oxide layer is destroyed by rub
radiation
Ideal blackbody radiation near melting is negligible compared to convection

## Slide 17
Higher performance turbomachinery reduces ignition margin
Design Choice | Benefit | Risk
higher turbine temperature | (more enthalpy change) | less margin to material and ignition limits
higher inlet pressure | (more pressure drop) | more severely oxidizing environment
smaller tip clearance | (less tip leakage) | higher rub risk
Design Choice | Benefit | Risk
higher turbine temperature |  | less margin to material and ignition limits
higher inlet pressure |  | more severely oxidizing environment
smaller tip clearance |  | higher rub risk

## Slide 18
Simulation bridges the gap between testing and in-engine conditions

## Slide 19
References [3]-[6]
blade
casing
Heat Transfer in Solids (ht)
initial conditions
cv
local CFD fields
oxidation
friction
convection
Coupled model implements transient frictional heating
interfacial constraints

## Slide 20
References [3]-[6]
imported CFD fields
initial conditions
Heat Transfer in Solids (ht)
K
Initial conditions set from CFD

## Slide 21
imported CFD fields
boundary conditions
References [3]-[6]
Heat Transfer in Solids (ht)
CFD results drive local boundary conditions

## Slide 22
imported CFD fields
boundary conditions
References [3]-[6]
Heat Transfer in Solids (ht)
CFD results drive local boundary conditions
Pa

## Slide 23
imported CFD fields
boundary conditions
References [3]-[6]
Heat Transfer in Solids (ht)
CFD results drive local boundary conditions
K

## Slide 24
Two-step approach to predict ignition
blade
casing
convection
and
oxidation
1. heatup
rubbing establishes thermal history.
convection
and
oxidation
blade
casing
2. ignition test
blade lifts. oxidation and convection at exposed surfaces.
friction
References [3]-[6]

## Slide 25
Aerojet AJ26 Rocket Engine - NASA
turbopump
rotor
blades
casing
model turbine
+
ignition
risk
turbine
rub
hot, high pressure O2
=
Why are oxygen-rich turbopumps vulnerable to frictional ignition?
25