## Slide 1: Microwave Annealer for Dopant Activation Above Solubility Limit
Jin Hong Joo1 and James C. M. Hwang1,2
1Department of Materials Science and Engineering, Cornell University
2School of Electrical and Computer Engineering, Cornell University
October 8th, 2026

## Slide 2: Outline
Introduction
COMSOL Multiphysics® Modelling and Optimization
Simulation Results
Prototype Microwave Annealer
Conclusion

## Slide 3: Semiconductor Microwave Annealing Using a Silicon Waveguide
Device Scaling and High Doping Level
Vacancy-Dopant Complexes
Dopant Activation
PV → P+ + e− + V
Source/Drain
(Si:P)
MOSFET
Smaller device dimensions require higher dopant concentrations to maintain good electrical performance
Excess dopants form vacancy–dopant complexes, degrading electrical performance
Microwave can dissociate dopant-defect complexes, releasing dopants and free electrons
Vacancy-dopant complex
Microwave annealing can reduce defect complexes and enhance electrical performance
→

## Slide 4: Semiconductor Microwave Annealing Using a Silicon Waveguide
Conventional Microwave Annealing
Annealing Through Silicon Waveguide
Silicon waveguide enables direct microwave coupling for efficient semiconductor annealing
Indirect heating through a susceptor
Nonuniform electric field and temperature distribution
Inefficient energy loss
Direct microwave-semiconductor interaction
Localized and uniform energy transfer
Enhanced dopant activation (25% more efficient; 6x more stable)

## Slide 5: COMSOL Modelling of the Microwave-Silicon Waveguide
Coaxial to Si Waveguide Transition
Simulation Geometry
Simulation Setup
Software | COMSOL Multiphysics® 6.2 and 6.3
Modules | RF module: Electromagnetic waves, Frequency Domain (ewfd) Heat Transfer Module: Heat Transfer in Solids (ht)
Frequency | 2.45 GHz (ISM Band)
Waveguide Design
Rectangular Si waveguide to interface with the Si sample
Designed to match dielectric properties and enable continuous wave propagation
Key Simulation Features
Mode transition: TEM in coaxial → TE10 in rectangular Si waveguide
Electric field concentration: maximum at the open end (sample interface)
Key Simulation Features
Coaxial
(TEM)
Transition
Si Waveguide
(TE10)
Open end
(Max |E|)
Si Sample
* Coaxial-to-waveguide coupling in Application Gallery

## Slide 6: Design Optimization with COMSOL Multiphysics®
Dual-Source
Single-Source
E-Field
STDEV
Each source w/ 1100W @ 2.45 GHz
Goal is to maximize the electric field at the sample (OPEN) while maintaining high uniformity
Maximum electric field occurs over a period of λSi/2
Swept key parameters, including source-coupling location and depth, and waveguide dimensions (width, height, thickness, etc.)
Design Optimization on Single- vs. Dual-Source
Phase Configuration
Sample
SHORT - 180°
(Out of Phase)
OPEN - 0°
(Same Phase)
MIN
MAX
Source
Si Waveguide
Si Waveguide
Si Waveguide
Top View
Source

## Slide 7: Simulation Results
Single-Source Design
Single- and dual-source designs to vary electric field intensity
Both designs maintain electric field uniformity within ± 5%
Dual-source design achieves 3.5x higher electric field intensity (420 vs. 120 V/cm)
Single-source maintains temperature of ~ 300 °C while dual-source reaches ~ 1000 °C
Dual-Source Design
Average electric field = 120 V/cm ± 5%
Average electric field = 420 V/cm ± 5%

## Slide 8: Prototype Microwave Annealer
Single-crystal Si boule machined into the designed rectangular waveguide
Household microwave oven modified to integrate the Si waveguide
Si waveguides enclosed by titanium (Ti) cladding and a heatsink for thermal management
Dual-Source Si Waveguide
Prototype Microwave Annealer
Single-Source Si Waveguide

## Slide 9: Prototype Microwave Annealer
Commercial Microwave Oven
Ti Waveguide
Cladding
Si Sample
Si Waveguide
Upgraded to a higher-power commercial microwave oven
Incorporated an isolator to minimize reflected microwave power
Implemented precise duty-cycle control for improved annealing control
Isolator Assembly
Isolator
Adaptor
Source

## Slide 10: Conclusion
Sheet Resistance Measurement Before and After MWA
 | Optimized the Si waveguide design using the RF and Heat Transfer modules in COMSOL Multiphysics®
 | Achieved simulated average electric fields of ~ 0.12 kV/cm ± 5.3% for the single-source and ~ 0.42 kV/cm ± 5.2% for dual-source
 | Preliminary MWA of P-doped Si above the equilibrium solubility limit reduced the sheet resistance from ~ 164 to ~ 144 Ω/□, corresponding to ~ 12% reduction.
 | The waveguide architecture can be scaled to larger samples by adjusting the waveguide dimensions and operating frequency
 | The approach is also being extended to other semiconductor materials, including GaN and Ga2O3.
Enhanced electrical performance

## Slide 11: Acknowledgement

## Slide 12: Thank you for listening! Questions?