## Slide 1
GREEN14
COMSOL CONFERENCE 2026 · CAMBRIDGE
Digital Twin of an Argon–Hydrogen Plasma Reactor
Bixente Artola
Senior Simulation Engineer
GREEN14 AB, Stockholm, Sweden

## Slide 2
GREEN14
2
INTRODUCTION · THE CHALLENGE
Europe's titanium leaves the continent as scrap
20 kt / yr
of Ti64 scrap exported from Europe or downcycled in 2025 — ~€160M of lost value
100 %
of Europe's virgin titanium sponge is imported — full dependence on Russia, China, Japan, Kazakhstan
1920s
when today's gas-atomization technology was designed — it only works with virgin feedstock
30–50 %
of conventional Ti64 powder production never makes Additive Manufacturing spec
Aerospace takes ~70 % of EU titanium demand — ~90 % of it is Ti64
Ti-6Al-4V — the aerospace workhorse alloy — is high value, tightly specified, and almost entirely imported.

## Slide 3
GREEN14
3
INTRODUCTION · THE PROJECT
One reactor: melt, reduce, atomize, quench
— Hydrogen plasma reactor. An arc-heated Ar/H₂ jet melts and chemically reduces scrap and out-of-spec powder — the only by-product is H₂O.
— Single step. Reduction, spheroidization and re-atomization happen in one pass: the supersonic nozzle breaks molten droplets and quenches them into spheres.
— Circular by design. Off-spec output and fines simply go back into the next run — zero waste powder, and ~5× lower CO₂ than conventional routes.
— Physical AI. Every run feeds our models and the models improve with every run — simulation and experiment sharpen each other. That loop is the rest of this talk.
IN — Ti64 scrap / out-of-spec
OUT — spherical Ti64
→
SEM of powder produced in the G14 reactor

## Slide 4
GREEN14
4
INTRODUCTION · GOALS
You cannot instrument a 12,000 K core
1
THE BLIND SPOT
No in-situ diagnostics
At ~10,000 K you cannot put a probe in the reaction zone — sensors sit far from the core, so simulation is the only way to reconstruct what each run actually did.
2
THE TWIN
COMSOL is the core solver
A multiphysics model of the chamber and nozzle rebuilds the full state of every run — temperature, flow, particles — from what the sensors can see at the walls.
3
THE FLYWHEEL
Every run sharpens the next
Simulate widely, run the most informative experiments, calibrate the twin on the results. Two hardware generations have already come out of this loop.

## Slide 5
GREEN14
5
METHODS · USE OF COMSOL MULTIPHYSICS
Three physics on one axisymmetric domain
— High Mach Number Flow, Turbulent SST. The Ar/H₂ plasma as a single LTE fluid, with properties tabulated from Cantera between 300 and 30,000 K, radiation as a net-emission sink, and Mach 0 to 3 in one domain.
— Conjugate heat transfer. The steel reaction chamber is resolved as a solid, and the helical cooling coil becomes a 1-D coolant equation along its curve — its contact conductance is the key unknown.
— Particle Tracing. Ti64 powder is traced through the frozen flow field — one-way coupling, justified because the loading is dilute.
— Small on purpose. About 65k elements, wall-resolved (Δw⁺ < 1); a transient solve takes ~20 min — fast enough to run thousands of times.
Axisymmetric domain: fluid + water-cooled walls, mesh refined at throat and walls
Water-cooled walls
Reaction chamber
Powder radial injection
Converging-Diverging nozzle

## Slide 6
GREEN14
8
METHODS · BEYOND THE BUILT-IN MODULES
A custom phase-change particle layer
— Full solid–liquid–vapor. Particle Tracing only ships with evaporation — we added melting through an effective heat capacity that carries the latent heat of fusion.
— Mach-dependent drag. Haider–Levenspiel below slip Mach 0.3 and Loth's compressible law above it, with the measured feedstock sphericity as the initial particle shape.
— KH/RT breakup. Molten droplets break up in the supersonic nozzle when the gas Weber number is large.
— Predicted product. Evaporation eats away the coarse tail — the median size drops from 58 to 47 µm — and irregular feedstock leaves as spheres.
Feedstock vs collected: volume PSD (left), sphericity vs diameter (right)

## Slide 7
GREEN14
6
METHODS · COMSOL ACROSS GREEN14
One platform, many models
1
PLASMA SOURCE
DC plasma torch
The gun itself is a separate COMSOL model — multifluid MHD in the Plasma Module.
2
COLLECTION
Cyclone separator
A particle-laden swirling-flow model used to design the cyclone that collects the product powder downstream of the nozzle.
3
HARDWARE
Water-cooled flange
Conjugate heat-transfer models of individual components — used to size the cooling channels so every flange survives its local heat load.
Shared foundations: every model is versioned in COMSOL Model Manager Server and built from our own parametric geometry-part library.
Workflow accelerated by AI: Claude drives COMSOL's Java API

## Slide 8
RESULTS · THE TWIN RUNNING
7
Gas temperature with streamlines (left) · Ti64 trajectories and the vapor source they release (right) — Ar 100 / H₂ 2.5 NLPM, ~22 kW
Particle injection through chamber and nozzle — colored by melting fraction (animation)

## Slide 9
GREEN14
9
RESULTS · OUR AI MACHINERY, EXPECTED VS. OBTAINED
Experimental data finds the unknowns
— Two unknowns — one example. The delivered inlet power and the coil-to-wall contact conductance — quantities no sensor can reach. The same machinery applies to any uncertain physical parameter.
— Two global observables. We match chamber pressure and coil heat — global, nearly independent quantities. Local thermocouples sit in gradients of ~15,000 K per cm, so they depend too much on exact placement.
— AI inverse solver. Unscented Kalman Inversion with Levenberg–Marquardt-style regularization — it treats COMSOL as a black box and runs cases in parallel on our server.
pressure 0.10 % · coil power 0.42 %
average match over 11 experiments — and the recovered inlet power tracks the measured net power even though it was never a fit target
Recovered inlet power vs measured net power (left); contact conductance ≈ 10 W/m²K across mixtures (right)

## Slide 10
GREEN14
10
CONCLUSIONS · IMPACT ON THE PROJECT
A calibrated twin is an instrument
1
OPERATING MARGINS
See what sensors cannot
The throat condensation state and the wall deposition rate warn of nozzle clogging before the throat actually narrows; the conjugate solution turns wall hot spots into a real safety margin for the chamber.
2
DESIGN
Optimize in software first
Geometry and operating points are screened in the twin before we build anything — two hardware generations have already come out of this loop.
3
AI LAYER
Toward live control
Learned source terms recover the missing physics as simple analytic expressions, and a neural surrogate wraps the calibrated twin so it answers in milliseconds — the path to self-supervised experiments.

## Slide 11
We take what the industry discards and upgrade it into its most valuable product by unlocking the value already embedded in the material.