## Slide 1
Uncertainty Quantification of
Bond-Front Velocity in
Direct Wafer Bonding
COMSOL Conference 2026 Shenzhen
Sichen Liang
School of Materials Science and Engineering, Sun Yat-sen University

## Slide 2
Presentation roadmap
Background
Bonding experiment and a three-layer device
04–05
Model and input domain
Coupled equations, adhesion and 12 inputs
07–09
Transient results
Mean front speed, height, displacement and pressure
11–13
Sensitivity analysis
Morris screening, Sobol indices and priorities
15–16
Conclusions
Main findings and acknowledgements
18
2

## Slide 3
Presentation roadmap
Background
Bonding experiment and a three-layer device
04–05
Model and input domain
Coupled equations, adhesion and 12 inputs
07–09
Transient results
Mean front speed, height, displacement and pressure
11–13
Sensitivity analysis
Morris screening, Sobol indices and priorities
15–16
Conclusions
Main findings and acknowledgements
18

## Slide 4
Contact growth
A local contact grows into a bonded region as the front advances.
Why speed matters
Q.Y. Tong and U. Gösele, Semiconductor Wafer Bonding: Science and Technology, 1998.
What controls mean bonding-front speed?
Mean front speed measures how fast bonded contact spreads across the wafer.
Background
Wafer bonding in experiment

## Slide 5
CEA-Leti demonstrator reported at IEEE ECTC 2024
3 layers
Two hybrid-bond interfaces
Face-to-face and face-to-back
4 and 6 µm pitch
Interface control becomes central as device layers accumulate.
S. Nicolas et al., 3-layer Fine Pitch Cu-Cu Hybrid Bonding Demonstrator With High Density TSV For Advanced CMOS Image Sensor Applications, ECTC, 2024.
Background

## Slide 6
Presentation roadmap
Background
Bonding experiment and a three-layer device
04–05
Model and input domain
Coupled equations, adhesion and 12 inputs
07–09
Transient results
Mean front speed, height, displacement and pressure
11–13
Sensitivity analysis
Morris screening, Sobol indices and priorities
15–16
Conclusions
Main findings and acknowledgements
18

## Slide 7
Thin plate deformation
Reynolds lubrication
Adhesion interaction
:wafer displacement [m]
: local gap [m]
: relative pressure [Pa]
: adhesive traction [Pa]
: gas viscosity [Pa·s]
Damien Radisson, Direct Bonding of Patterned Surfaces, Grenoble university, PhD thesis, 2014.
Model and input domain
Governing relation and outputs
Notes: The two small boxes at the lower right are reserved for the project-specific COMSOL bonding-wave propagation clip and overall bonding-process clip. An external infrared bonding-wave sequence appears beside the coupled model. Governing equations shown in the first version include plate flexural rigidity D = E t_w^3 / [12(1 - ν^2)] and v_bond = d r_bond / dt over stable propagation.

## Slide 8
Damien Radisson, Direct Bonding of Patterned Surfaces, Grenoble university, PhD thesis, 2014.
: well depth [J/m²]
: interaction length [m]
: equilibrium gap [m]
Well depth
sets the adhesion energy per unit area.
Equilibrium separation
is the gap at the energy minimum.
Interaction range
determines how quickly the force changes with separation.
Model and input domain
Adhesion potential well
Notes: Figure basis: Damien Radisson, Direct Bonding of Patterned Surfaces, PhD thesis (2014), Figure 3, captioned “Plot of the potential energy well and its derived conservative attraction force.” The source figure is listed at https://www.researchgate.net/figure/Plot-of-the-potential-energy-well-and-its-derived-conservative-attraction-force_fig3_279534609 . This editable redraw is qualitative and is not digitized from the thesis. F = -dU/dh is the conservative-force relation; positive force is defined here as increasing the surface gap. The sketch has no numeric scales or fitted potential law.

## Slide 9
Twelve material, interface and cavity inputs define the study domain
Mechanics & material
Interface & gap
Cavity design
1
Input domain
12 inputs
2
MOAT screening
Rank effects
3
Select key inputs
Reduce input
4
Train surrogate
Selected surrogate
5
Sobol analysis
SI and ST effects
Wafer
thickness
t
w
200–775 µm
Young’s modulus E
110–180 GPa
Poisson’s ratio ν
0.28–0.35
Density ρ
2330–3000 kg/m³
Adhesion energy Eₐ
0.02–0.10 J/m²
Interaction range β
5–30 nm
Gas viscosity μ
1.6–2.1 × 10⁻⁵ Pa·s
Blade
thickness
t
b
50–300 µm
Cavity
depth
d
Inner
radius
r
in
Outer
radius
r
out
Cavity
angular
width
Δφ
g
2–15°
0.1–10 µm
0–20 mm
80–100 mm
Input domain and uncertainty workflow
Notes: Author confirmation needed: define β and t_b physically; cite the source and probability distribution for each uncertain input; confirm whether inputs are independent.

## Slide 10
Presentation roadmap
Background
Bonding experiment and a three-layer device
04–05
Model and input domain
Coupled equations, adhesion and 12 inputs
07–09
Transient results
Mean front speed, height, displacement and pressure
11–13
Sensitivity analysis
Morris screening, Sobol indices and priorities
15–16
Conclusions
Main findings and acknowledgements
18

## Slide 11
Bonding front propagation
Upper wafer deformation
Transient results
Bonding dynamics and front speed

## Slide 12
Fast initial decrease, a small rebound near 1.5–2 s, then a near-zero tail by about 8.5 s.
Observed evolution
Fast initial decrease, a small rebound near 1.5–2 s, then a near-zero tail by about 8.5 s.
Local bonding velocity
vbonding(t) = dSf/dt
Sf is the moving front position.
Transient results
Upper-wafer closure dynamics
Notes: The source plot labels its ordinate as dependent variable u (m). Confirm whether this is vertical displacement u_z at the stated upper-wafer probe before relabeling it.

## Slide 13
Bonding-face displacement
The bright radial lobes mark regions with larger displacement of the upper bonding face.
Physical meaning
Localized vertical deformation changes wafer separation and affects gas drainage.
Transient results
Deformation of the cavitied wafer
Notes: Author confirmation required: displacement component, physical unit, time point, and groove orientation. The embedded color scale shows ×10⁻⁷ but has no unit.

## Slide 14
Presentation roadmap
Background
Bonding experiment and a three-layer device
04–05
Model and input domain
Coupled equations, adhesion and 12 inputs
07–09
Transient results
Mean front speed, height, displacement and pressure
11–13
Sensitivity analysis
Morris screening, Sobol indices and priorities
15–16
Conclusions
Main findings and acknowledgements
18

## Slide 15
Cavity depth, outer radius, wafer thickness and groove angle show moderate effects.
Smaller effects
The remaining inputs have smaller elementary effects within this input domain.
Largest effects
Intermediate effects
Adhesion energy Eₐ and interaction range β lie in the upper-right part of the plot.
Sensitivity analysis
Morris sensitivity screening
Notes: Add numerical μ* and σ values or uncertainty bounds if available. Define the aggregation used for “others.”

## Slide 16
0.63
ST for cavity depth
0.24
ST for adhesion energy
0.21
ST for angular width
Sensitivity analysis
Sobol sensitivity results
Notes: Add confidence intervals or bootstrap ranges, surrogate validation error, and exact Monte Carlo/Sobol sample counts.

## Slide 17
Presentation roadmap
Background
Bonding experiment and a three-layer device
04–05
Model and input domain
Coupled equations, adhesion and 12 inputs
07–09
Transient results
Mean front speed, height, displacement and pressure
11–13
Sensitivity analysis
Morris screening, Sobol indices and priorities
15–16
Conclusions
Main findings and acknowledgements
18

## Slide 18
Results
Sobol sensitivity results
Sobol total effect
0.63
Cavity depth has the largest reported total effect.
Morris screening
Eₐ, β
Adhesion energy and interaction range show the largest screening effects.
Wafer mechanics
Thickness
Wafer thickness shows an intermediate Morris effect.

## Slide 19
This work was financially supported by the National Natural Science Foundation of China under grant number 51832002 and the National Science and Technology Major Project of China under grant number 2024ZD0607800. The authors also gratefully acknowledge Dr. G. Wang of COMSOL China for technical support.
Thanks for Your Attention!
Contact email: liangsch5@mail2.sysu.edu.cn
Sichen Liang
Notes: Validation status: the supplied deck reports no mesh/time-step convergence results or independent physical validation data. Keep this limitation visible when presenting predictive claims.